Optical vs tactile surface metrology: multi-material analysis of measurement error and wavelength effects

D. Kucharski1*[0000-1111-2222-3333], Second Author1[1111-2222-3333-4444], and Third Author2[2222-3333-4444-5555]

1Affiliation, Town/City, Country
firstname.secondname@springernature.com

Keywords: First Keyword, Second Keyword, Third Keyword.

# Extended Abstract

The present study evaluates the agreement between optical surface metrology systems and a tactile reference across a range of roughness parameters, materials, and finishing processes (see, e.g., Figure 1). The main objective is to quantify the absolute percentage error of optical measurements relative to the tactile baseline and to identify which factors – optical system, colour (as a proxy for illumination wavelength), roughness parameter, and material/process – have the greatest influence on this error. The analysis is intended to support practical recommendations for selecting optical configurations that approximate tactile measurements as closely as possible in industrial use.

Measurements were taken for various engineering materials and machining or finishing processes, using a standard set of roughness parameters (e.g., Ra, Rz, Rt, Rz1max, Rp, Rv). Tactile data were initially cleaned using automatic header detection and numeric parsing; the tactile reference for each case was set to the average tactile value for the corresponding parameter. Optical data were parsed to determine the system identity, colour channel, and nominal wavelength for each measurement. For each observation, the absolute percentage difference was calculated as

diff%=100⋅O-SS,

where O represents the optical value and S the tactile reference, and all subsequent analyses were conducted on this absolute error. Figure 1 summarises the mean absolute percentage error for all optical systems across the dataset, highlighting significant performance variations between systems.

The statistical workflow combined several complementary components. First, for each material/process and parameter, an analysis of variance of |diff| (%) was carried out with system and colour as fixed factors, using the schematic model
diff%=system+color+ε,

and yielding eta-squared effect sizes for both factors. These results were summarised by “effects by system” and “effects by colour” plots, and by tables of mean errors with 95% confidence intervals. Second, possible wavelength dependence was examined by global Pearson and Spearman correlations between |diff| (%) and wavelength and, more importantly, by linear regressions fitted separately for each system, modelling
diff%=β0+β1⋅wavelength+ε.
For every system the estimated slope β1, its confidence interval and p-value were reported, and systems with statistically significant slopes (p < 0.05) were flagged; additional “trend” cases with 0.05 ≤p < 0.1 were recorded. Third, “technical distance” heatmaps were constructed from matrices of mean absolute percentage differences between systems, providing a visual summary of how similar or dissimilar different optical configurations are to one another and to the tactile reference. A representative case of close agreement between optics and the tactile reference for one material/parameter combination is shown in Figure 2.

To obtain a more comprehensive ranking of influential factors, the statistical analysis was complemented by machine learning models trained to predict |diff| (%) from categorical descriptors (system, colour, parameter, and material/process). Lasso and Ridge regression (via GLMNET) were used to derive coefficient-based importance scores, while Random Forest models provided permutation importances and SHAP value summaries. These models were fitted to both the full data set and to subsets split by parameter or by material/process. An extended cross-validation scheme, including hyperparameter tuning for GLMNET and Random Forest, was used to assess robustness; aggregated performance metrics and importance tables were reported for all folds.

Across materials and parameters, the results show that the choice of optical system is usually the main factor influencing the error, with colour having a secondary but sometimes significant impact. Eta-squared values for the system factor are often larger than those for colour, and the best system for a particular parameter/material combination often achieves considerably lower mean |diff| (%) than the worst one. However, for several materials and parameters, the analyses also reveal statistically significant slopes of |diff| (%) with respect to wavelength in at least one system, indicating that wavelength-related effects cannot be ignored. Figure 3 illustrates such a case, showing how |diff| (%) depends on wavelength and the related slopes for each system. The parameter-specific summaries show that some roughness metrics display more frequent and stronger wavelength dependence than others, and that the maximum eta-squared values for system and colour vary systematically across parameters. The machine-learning models support these findings: in both global and parameter-specific settings, system indicators consistently rank among the most important predictors of error, with colour and, to a lesser extent, material or process also playing significant roles. The advanced cross-validation confirms that these importance rankings remain stable when resampling.

From an application perspective, the combined evidence enables the development of synthetic recommendations. For each material and parameter, the report identifies the system with the lowest mean absolute percentage error, the most favourable colour channel, and – where available – the optimal system–colour pair. Qualitative trend descriptions summarise whether error tends to increase or decrease with wavelength for the most informative system, and whether other systems exhibit weaker but noteworthy tendencies. A representative technical distance heatmap (see Figure 4) reveals clusters of similar systems and clear outliers, supporting practical configuration grouping and identifying those requiring special attention.

In summary, the study shows that, for many combinations of roughness parameter and material or process, carefully chosen optical systems can achieve errors that are small and stable enough to act as practical substitutes for tactile measurements. However, the strong influence of system choice, the significant role of colour, and the presence of notable wavelength trends in several settings highlight the need for system- and parameter-specific validation rather than assuming uniform behaviour across different configurations. The combined use of ANOVA, regression, “technical distance” mapping, and machine learning importance analysis offers a comprehensive framework for such validation and for developing evidence-based recommendations for industrial metrology practice.

Figure 1. Main effects of measurement system on absolute roughness error |diff| (%) for Ra on Ti6Al4V after micro‑finishing.

Figure 2. Comparison of |diff| (%) for Ra on Ti6Al4V after micro‑finishing obtained from optical systems versus the tactile reference.

Figure 3. Dependence of absolute roughness error |diff| (%) for Ra on Ti6Al4V after micro‑finishing on the illumination wavelength for individual optical systems

Figure 4. Technical distance matrix between optical and tactile systems for Ra on Ti6Al4V after micro‑finishing, based on mean absolute roughness error |diff| (%)